FLAGSHIP — DECORATIVE PAVEMENT MARKING SYSTEM

# TrafficPatternsXD

Manufacturer: Ennis-Flint® by PPG (PPG Traffic Solutions, Greensboro NC). HUBSS is the Canadian distributor and certified-applicator network.

PURPOSE OF THIS DOCUMENT

Source-of-truth reference for HUBSS website product copy. Replaces existing website descriptions that have been flagged as inaccurate or embellished. Doug Bain to review, correct, and sign off — every claim on the website must be supported by a fact listed in this document.

## What it is

An imprinted, aggregate-reinforced preformed thermoplastic pavement marking system. Two-foot-square sheets are laid on prepared asphalt, heated, and stamped with a wire-rope template — producing a brick-style decorative crosswalk or traffic-calming surface that is permanently bonded to the asphalt below.

The 'XD' stands for 'Extremely Durable.' TrafficPatternsXD is the heavy-duty variant of the TrafficPatterns family, engineered for the most demanding pedestrian and vehicular conditions — bus lanes, BRT corridors, high-volume intersections.

## Key features

- 150 mil (3.8 mm) minimum thickness — heaviest in the preformed thermoplastic line.

- Aggregate-reinforced through the full cross-section; new anti-skid elements are exposed as the surface wears.

- Sheets stamped into the asphalt with a wire-rope template after heating — produces a brick-style imprinted finish.

- Heat-fused to asphalt — permanent chemical bond, not a coating that can peel.

- Applies at ambient and road temperatures down to 45°F (7°C); no pavement preheating to a specific temperature required.

- Available in 25+ standard colours plus a premium palette (PMS values published in the Colour Guide).

## Technical specifications

| Material | Preformed thermoplastic — ester-modified rosin, aggregates, pigments, binders, anti-skid elements |
| --- | --- |
| Minimum thickness | 150 mil (3.8 mm) |
| Sheet size | 2 ft × 2 ft (0.61 m × 0.61 m), ±3 mm tolerance |
| Anti-skid (intermixed) | Minimum 30% intermix; minimum 6 Mohs hardness |
| Skid resistance | Minimum 60 BPN per ASTM E303 |
| Static friction | Minimum 0.6 (wet & dry) per ASTM C1028 / ASTM D2047 |
| Minimum install temperature | 45°F (7°C) ambient and road |
| Substrate | Asphalt only — explicitly NOT for Portland cement concrete |
| Retroreflectivity | Non-reflective. Companion white transverse stripe (90 / 125 mil) carries glass beads if required. |
| Storage | 24 months indoors |
| Sealer | Two-part epoxy required prior to application — no VOC solvents; gel time ≥ 20 min at 27°C |
| Carton | Max 25 in × 25 in; max 70 lb (32 kg) |

## Colours / palette

25+ standard colours including Black, White, Field Grey, Grey, Salmon, Sonoma Sand, Cinnamon, Sienna, Cocoa, Heritage Red, Colonial Brick, Burnt Orange, Terracotta, Khaki, Tan, Sand, Santa Fe Clay, Chestnut, Dark Brick Red, Brick Red, Light Grey, Olive Green, Green, Pink, Purple, Lilac. Premium colours: Light Blue, Sky Blue, Blue, Teal, SYG, Kelly Green, Lemon Yellow, Light Green, Orange, Yellow, Red. Pantone references are published in the Colour Guide. Custom patterns and colours available on request, within manufacturing limits.

## Applications & ideal use-cases

- High-volume decorative crosswalks

- BRT corridors and bus priority lanes

- Major intersections subject to heavy turning movements and concentrated wheel loads

- Traffic-calming installations on collector and arterial streets

- Civic plazas with vehicular access through the area

- Through-areas in parking lots

## Document library

Current document set for this product. Proposed clean titles below — fixes duplicate / generic naming on the current site.

| Document title | Type | File |
| --- | --- | --- |
| Product Specification | Specification | TrafficPatternsXD-Specification.pdf |
| Product Specification (branded HUBSS cover) | Specification | TrafficPatternsXD-Specification-Branded.pdf |
| Product Specification (French) | Specification (FR) | TrafficPatternsXD-Specification-FR.pdf |
| Two-Component Sealer Specification | Specification | TrafficPatternsXD-Two-Component-Sealer.pdf |
| Cross-Section Detail | Drawing | TrafficPatternsXD-CrossSection-Detail.pdf |
| Colour Guide | Colour Guide | TrafficPatternsXD-Colour-Guide.pdf |
| Technical Data Sheet (TS002) | TDS | TS002_TrafficPatternsXD_220204.pdf |
| Design Manual | Design Manual | TrafficPatternsXD-Design-Manual.pdf |

## Source notes & [VERIFY] flags

SOURCES USED

- TrafficPatternsXD Specification (.pdf)

- TrafficPatternsXD TS002 Technical Data Sheet (.pdf)

- TrafficPatternsXD Cross-Section Detail (.pdf)

- TrafficPatternsXD Colour Guide (.pdf)

- TrafficPatternsXD Two-Component Sealer Specification (.pdf)

- PPG Traffic Solutions launch announcement, January 2021 (PCI Magazine / PPG investor relations)

ITEMS REQUIRING DOUG'S CONFIRMATION

[VERIFY] Open-to-traffic time after installation: the spec says "allowed to cool thoroughly" but does not state a specific number of minutes or hours. The current site claim of "open to traffic within hours" is plausible but unsourced — confirm the practical re-opening time for a typical installation.

[VERIFY] Coverage rate: TPXD is sold per panel/sheet rather than per area. Confirm what HUBSS quotes to municipalities — sq ft per panel? installed sq ft per crew-day?

[VERIFY] AODA compliance: the technical data sheet cites ADA compliance specifically (American). AODA is not referenced anywhere in the PPG / Ennis-Flint documentation. Confirm whether HUBSS has independent AODA test data or should reword as "designed to meet accessibility standards including ADA; suitable for AODA-compliant designs subject to site-specific review."

[VERIFY] Service life: PDFs do not state a specific year-figure for TPXD service life. Website language like "engineered for multi-year service" is defensible; specific claims like "20-year durability" or "7-year service life" are not in any source document — supply project-based evidence if those claims are to appear on the site.

CURRENT SITE COPY FLAGGED AS INACCURATE / EMBELLISHED

[VERIFY] Current website specs claim "Glass beads embedded through full cross-section" — this is INCORRECT for TPXD. The technical data sheet describes anti-skid/anti-slip elements (minimum 30% intermix, minimum 6 Mohs hardness), NOT glass beads. Glass beads only apply to the companion white transverse stripe and to PreMark's beaded variants. Recommended correction: "Anti-skid elements distributed through full cross-section — new elements exposed as the surface wears."

[VERIFY] Current website claims TPXD installs on "asphalt or concrete." PDF specification §5.4 is explicit: "The System shall not be applied to Portland Cement Concrete." Asphalt only.

[VERIFY] Current website document list shows THREE entries all labeled "Specification" (Branded, plain English, and French). Proposed clean titles: "Product Specification" / "Product Specification (branded HUBSS cover)" / "Product Specification (French)" — each visually distinct and meaningful to the reader.

Approved for website use by: ______________________________   Date: ______________