FLAGSHIP — SOLAR-REFLECTIVE PAVEMENT COATING

# StreetBondSR

Manufacturer: GAF / StreetBond (Parsippany NJ). Same parent product family as StreetBond. HUBSS is the Canadian distributor.

PURPOSE OF THIS DOCUMENT

Source-of-truth reference for HUBSS website product copy. Replaces existing website descriptions that have been flagged as inaccurate or embellished. Doug Bain to review, correct, and sign off — every claim on the website must be supported by a fact listed in this document.

## What it is

Solar-reflective version of StreetBond150 — the standard waterborne epoxy-modified acrylic coating is paired with high-SRI pigment colourants to reduce surface temperature and mitigate urban heat island effects.

Engineered specifically for projects targeting LEED v4 Sustainable Sites Credit 7.1 (Heat Island Effect — Non-Roof), climate action plan implementation, or municipal heat-mitigation programs.

## Key features

- Solar Reflectance Index (SRI) ≥ 29 qualifies for LEED credit — multiple StreetBondSR colours documented above this threshold.

- 'Invisible Shade' colourant technology pushes Solar Reflectance > 0.334 — meeting LEED thresholds without restricting designs to white or light grey only.

- Same flexible adhesion + slip-resistance characteristics as StreetBond150 — the SR effect is achieved through colourant chemistry, not by changing the base coating.

- Documented compliance with LEED v4 SSc7.1 (Heat Island Effect) and Green Neighborhood Development GIB Credit 9.

- Manufactured in ISO 9001 and ISO 14001 facilities.

## Technical specifications

| Base coating | StreetBond150 (waterborne epoxy-modified acrylic) |
| --- | --- |
| Volume solids | 58.2% (ASTM D2697) |
| Weight solids | 74.9% (ASTM D2369) |
| Density | 13.8 lbs/gal (1.58 kg/L) per ASTM D1475 |
| Shore hardness | 38.3 (ASTM D2240) |
| VOC | Approx. 19 g/L measured (ASTM D3960-05) — well below SCAQMD Rule 1113 thresholds |
| Friction — wet | 77 BPN (ASTM E303) |
| Friction — dry | 81 BPN (ASTM E303) |
| Solar Reflectance Index | Limestone Grey SRI = 65; Slate SRI = 33; multiple other SR-qualifying colours |
| Solar Reflectance (SR, distinct from SRI) | ≥ 0.334 with Invisible Shade colourants |
| LEED credit | SSc7.1 Heat Island Effect (Non-Roof) — 1 credit at SRI ≥ 29 on ≥ 50% of hardscape |
| Flexibility (mandrel bend) | Passes 6.35 mm @ 21°C; passes 101.6 mm @ -18°C |
| Drying — re-coat | 35 min at 23°C, 37% RH (ASTM D5895) |

## Colours / palette

Same overall StreetBond palette (73+ colours), with SR-qualifying colours flagged in the StreetBondSR Colour Guide. Documented SR values include Marigold 0.35, Avocado 0.35, Pumpkin Spice 0.33, Chestnut Brown 0.34, Limestone Grey SRI 65, Slate SRI 33.

## Applications & ideal use-cases

- Parking lots targeting LEED Heat Island Reduction credit

- Civic plazas and pedestrian-priority areas in climate-action zones

- School and campus hardscape (children's surface temperature exposure)

- Urban parks and pathways in heat-vulnerable communities

- Commercial sites with sustainability reporting requirements

## Document library

Current document set for this product. Proposed clean titles below — fixes duplicate / generic naming on the current site.

| Document title | Type | File |
| --- | --- | --- |
| StreetBondSR Brochure | Brochure | StreetBondSR-Brochure.pdf |
| Colour Guide — SR-qualifying tones | Colour Guide | Colour-Guide-1.pdf |
| Friction Certificate of Analysis (ASTM E303) | Certificate | StreetBond-SR-Certificate-of-Analysis-Friction.pdf |
| Flat Surface Product Specification | Specification | StreetBond-SR-Flat-Surface-Specification.pdf |

## Source notes & [VERIFY] flags

SOURCES USED

- StreetBondSR Brochure and Flat Surface Specification (.pdf)

- StreetBondSR Friction Certificate of Analysis — GeoEngineers (.pdf)

- StreetBondSR Colour Guide (.pdf)

ITEMS REQUIRING DOUG'S CONFIRMATION

[VERIFY] Current site spec reads "Initial Solar Reflectance ≥ 0.33" — defensible, but the technical foundation is actually SRI ≥ 29 (the LEED-credit metric). SR and SRI are related but different scales. Recommend stating BOTH: "SRI ≥ 29 (LEED qualifying) / Solar Reflectance > 0.334 with Invisible Shade colourants."

[VERIFY] LEED credit name — "SS Credit: Heat Island Reduction" is current LEED v4 language; LEED v4.1 may use updated nomenclature. Confirm the current credit label HUBSS wants on the site.

[VERIFY] Coverage / dry time / cure are inherited from StreetBond150 — confirm they should be listed on the SR page directly or referenced back to the StreetBond page.

CURRENT SITE COPY FLAGGED AS INACCURATE / EMBELLISHED

[VERIFY] Current site lists Solar Reflectance ≥ 0.33 as a flat number. The SR test value documented in the materials is ≥ 0.334. More importantly, the LEED requirement is SRI ≥ 29 (a different, more rigorous metric). The site should reflect the LEED metric directly.

[VERIFY] Document library on the current site does not show the Friction Certificate of Analysis prominently — for LEED submissions and municipal procurement, this is one of the most useful documents to feature, since it documents both slip resistance AND VOC compliance in one place.

Approved for website use by: ______________________________   Date: ______________