CONCRETE & ASPHALT REPAIR

# Fast Patch DPR

Manufacturer: FastPatch® is a registered trademark of The Willamette Valley Company LLC (USA), marketed through FastPatch Systems (fastpatchsystems.com) and PavePatch.com. Distributed in Canada by HUB Surface Systems. NOTE: Fast Patch DPR is a Willamette Valley Company product, NOT a HUB-manufactured product.

PURPOSE OF THIS DOCUMENT

Source-of-truth reference for HUBSS website product copy. Replaces existing website descriptions that have been flagged as inaccurate or embellished. Doug Bain to review, correct, and sign off — every claim on the website must be supported by a fact listed in this document.

## What it is

FastPatch DPR (Distressed Pavement Repair) is a polymer-blend pourable repair material for asphalt and concrete — engineered for high-strength, fast-return-to-service repair of potholes, spalls, joints, wheel paths, and utility cuts. Mixed with a cordless drill, poured into the defect, and back in service in less than 45 minutes.

Made from a unique polymer blend with up to 80% recycled and renewable materials (manufacturer claim). Odourless — suitable for indoor environments where ventilation rules out hot-mix or solvent-based materials.

## Key features

- Back in service in less than 45 minutes (1 hr at 75°F, 2–3 hr at 50–65°F).

- FastPatch Kicker accelerator available for cooler-weather work — shortens cure time further.

- 100% solids, 80% recycled/renewable polymer matrix.

- Completely odourless — suitable for warehouse floors, loading docks, and underground parking where ventilation constraints exclude petroleum-based materials.

- Excellent freeze-thaw resistance and impact absorption.

- Snowplow-friendly.

- Available in asphalt-repair formulation and concrete-repair formulation.

- Pre-measured kits: 5-gallon (11 L), 3-gallon (5 L), 1-gallon (2.5 L).

## Technical specifications

| Type | Polymer-blend distressed pavement repair material |
| --- | --- |
| Composition | Polymer matrix with up to 80% recycled and renewable materials; 100% solids |
| Application method | Mix with cordless drill, pour, finish |
| Cure time at 75°F (24°C) | 1 hour |
| Cure time at 50–65°F (10–18°C) | 2–3 hours |
| Return to service | < 45 minutes (with appropriate temperature/accelerator) |
| Cold-weather option | FastPatch Kicker accelerator |
| Substrate | Asphalt and concrete (separate formulations available) |
| Kit sizes | 5 gal (11 L) / 3 gal (5 L) / 1 gal (2.5 L) pre-measured kits |
| Odour | Odourless — suitable for indoor application |
| Freeze-thaw resistance | Excellent (manufacturer claim) |
| Snowplow compatibility | Snow-plow friendly |
| VOC | [Not stated on FastPatch product page — VERIFY] |
| Manufacturer | The Willamette Valley Company LLC (USA) |

## Colours / palette

Black (asphalt formulation) and concrete-grey (concrete formulation). Not a decorative product.

## Applications & ideal use-cases

- Roadways and bridges — spalls, crack repair, joint repair, broken corners, surface leveling, potholes

- Airports — spalls, wheel-path areas, approaches and departures

- Parking lots — potholes, walkways, broken areas

- Warehouses — floor spalls, loading-dock areas

- Sidewalks and curbs — trip-hazard remediation, walkway repair

- Indoor environments where ventilation constraints exclude solvent or asphalt-emulsion products

## Source notes & [VERIFY] flags

SOURCES USED

- FastPatch Systems — FastPatch DPR product page (https://fastpatchsystems.com/fastpatch-dpr/)

- PavePatch.com — FASTPATCH product overview (https://www.pavepatch.com/fastpatch-product-overview-i-18.html)

- Amazon product page — FASTPATCH DPR Pourable Asphalt Repair 5-Gal Kit

ITEMS REQUIRING DOUG'S CONFIRMATION

[VERIFY] CRITICAL: Manufacturer attribution. Fast Patch DPR is The Willamette Valley Company LLC, marketed through FastPatch Systems. The current HUBSS website does not attribute this. Confirm whether HUBSS holds a Canadian distribution arrangement and how the website should display manufacturer attribution.

[VERIFY] There are NO PDFs in /public/docs/fast-patch/ — the site has no document downloads. Recommend sourcing the FastPatch DPR TDS, MSDS/SDS, application instructions, and Kicker product literature from FastPatch Systems.

[VERIFY] VOC value, exact freeze-thaw cycle count, ASTM test data, and specific compliance certifications are not enumerated on the manufacturer's public product page. Source from the TDS / SDS.

[VERIFY] "Up to 80% recycled and renewable materials" — manufacturer claim. Confirm before quoting the specific 80% figure on the HUBSS site (the figure varies kit-to-kit per manufacturer marketing).

[VERIFY] FastPatch DPR is sold under the FastPatch® brand. Confirm whether HUBSS website should use "Fast Patch DPR" (current site) or "FASTPATCH® DPR" (manufacturer style) — trademark display matters.

CURRENT SITE COPY FLAGGED AS INACCURATE / EMBELLISHED

[VERIFY] Current site presents Fast Patch DPR as a HUB-distributed product without manufacturer attribution. The product is a registered trademark of Willamette Valley Company / FastPatch Systems and is distributed by several US/Canadian retailers — exclusive Canadian distribution arrangement (if any) should be confirmed and visible.

[VERIFY] Current site claims "completely odourless, making it suitable for indoor environments including warehouse floors, loading docks, and underground parkades." Manufacturer confirms odourless + indoor suitability — claim is supported.

Approved for website use by: ______________________________   Date: ______________