FLAGSHIP — DECORATIVE PAVEMENT MARKING SYSTEM

# TrafficPatterns

Manufacturer: Ennis-Flint® by PPG (PPG Traffic Solutions, Greensboro NC). HUBSS is the Canadian distributor and certified-applicator network.

PURPOSE OF THIS DOCUMENT

Source-of-truth reference for HUBSS website product copy. Replaces existing website descriptions that have been flagged as inaccurate or embellished. Doug Bain to review, correct, and sign off — every claim on the website must be supported by a fact listed in this document.

## What it is

An interconnected preformed thermoplastic pavement marking system that simulates pavers or stones. Pre-cut interlocking sheets are surface-applied with infrared heat — no stamping templates or grids required.

The standard-duty product in the TrafficPatterns family. Suitable for decorative crosswalks, parks, schools, and public spaces where TPXD's heavier 150 mil cross-section is not required. Works on BOTH asphalt and concrete — a key differentiator from TPXD.

## Key features

- 125 mil (3.2 mm) minimum thickness — preformed at the factory.

- Interconnected sheet design simulates pavers; no stamping template required (unlike TPXD or StreetPrint).

- Applies to both asphalt AND Portland cement concrete, including 'green' concrete that has set but not appreciably hardened.

- Heat-applied with an infrared heater — heating indicators on the surface signal molten state.

- Anti-skid elements harder than TPXD — minimum 8 Mohs (vs. 6 Mohs for TPXD).

- 'Open to traffic within minutes of application' (manufacturer marketing language).

## Technical specifications

| Material | Preformed thermoplastic — ester-modified rosin, aggregates, pigments, binders, anti-skid elements |
| --- | --- |
| Minimum thickness | 125 mil (3.18 mm) |
| Sheet size | Interconnected: 24 in × 24 in (0.61 × 0.61 m). Solid Sheets variant: 24 in × 36 in (0.61 × 0.91 m) |
| Anti-skid (intermixed) | Minimum 30% intermix; minimum 8 Mohs hardness |
| Skid resistance | Minimum 60 BPN per ASTM E303 |
| Static friction | Minimum 0.6 (wet & dry) per ASTM C1028 / ASTM D2047 |
| Minimum install temperature | 45°F (7.2°C) ambient and road |
| Substrate | Asphalt AND Portland cement concrete (including green concrete) |
| Installation | Infrared heat — no stamping template, no grid |
| Carton | Max 25 in (Solid: 40 in) × 25 in; max 50 lb (23 kg) |

## Colours / palette

Same standard + premium palette as TrafficPatternsXD (see TPXD entry). Standard patterns: Running Bond, Herringbone, Plain Weave, Basket Weave, Ashlar, Stacked Tile (large + small), Diagonal Tile (large + small), Honeycomb, Courtyard, Quarter Round, Terrazzo. Standard borders TP36 through TP42.

## Applications & ideal use-cases

- Decorative crosswalks (standard duty)

- Parks and pathways

- Schools and playgrounds (regulatory + decorative)

- Public spaces and civic plazas

- Parking lot through-areas and design elements

- Pedestrian-safety treatments where TPXD's heavier 150 mil is not required

## Document library

Current document set for this product. Proposed clean titles below — fixes duplicate / generic naming on the current site.

| Document title | Type | File |
| --- | --- | --- |
| Product Specification — Solid Sheets 125 mil | Specification | TrafficPatterns-Solid-Sheets-125-Specification.pdf |
| Product Specification — 125 mil with Self-Adhesive Back | Specification | TrafficPatterns-125-with-SA-Specification.pdf |
| Two-Component Sealer Specification | Specification | TrafficPatterns-Specification-Two-Component-Sealer.pdf |
| Custom Design Guidelines | Design Guide | TrafficPatterns-Custom-Design-Guidelines.pdf |
| Colour Guidelines | Colour Guide | TrafficPatterns-Colour-Guidelines.pdf |
| Technical Data Sheet (TS001) | TDS | TS001_TrafficPatterns_220204.pdf |
| Design Manual | Design Manual | TrafficPatterns-Design-Manual.pdf |

## Source notes & [VERIFY] flags

SOURCES USED

- TrafficPatterns Solid Sheets 125 Specification (.pdf)

- TrafficPatterns 125 with Self-Adhesive Specification (.pdf)

- TrafficPatterns TS001 Technical Data Sheet (.pdf)

- TrafficPatterns Colour Guidelines (.pdf)

ITEMS REQUIRING DOUG'S CONFIRMATION

[VERIFY] "Glass beads embedded through full cross-section" appears on the current site — same correction as for TPXD. TrafficPatterns carries anti-skid elements, not glass beads, through the cross-section. Glass beads are a PreMark feature, not a TrafficPatterns one.

[VERIFY] "Open to traffic in hours" — TS001 says "within minutes." Confirm with HUBSS whether "minutes" applies to small areas (a single crosswalk) vs. "hours" for large-area installations.

[VERIFY] Pedestrian-safety / freeze-thaw resilience: claims are reasonable but not quantified in the PDFs. If specific year-figures are used on the site ("holds retroreflectivity for years"), they should be qualified — TrafficPatterns is a non-reflective product; the retroreflectivity claim more accurately belongs to PreMark or the companion white transverse stripe.

CURRENT SITE COPY FLAGGED AS INACCURATE / EMBELLISHED

[VERIFY] Current website: "Retroreflective glass beads are embedded through the full cross-section, holding nighttime visibility as the surface wears." — INCORRECT for TrafficPatterns. The product contains anti-skid elements at minimum 8 Mohs hardness; it is described by the manufacturer as a decorative product, not a retroreflective one. Retroreflectivity is provided by accompanying white transverse stripes (separate product line) or by PreMark beaded variants.

[VERIFY] Current website says "holds retroreflectivity for years where conventional traffic paint typically requires repainting in a year or less." — overstatement. Reword as decorative durability vs. paint durability.

[VERIFY] Current document library has "Two-Component Sealer Spec" and three other specs without strong differentiating labels. Proposed clean titles above remove ambiguity.

Approved for website use by: ______________________________   Date: ______________