FLAGSHIP — COLOURED PAVEMENT COATING SYSTEM

# StreetBond

Manufacturer: GAF / StreetBond (1 Campus Drive, Parsippany-Troy Hills, NJ 07054). NOT an Ennis-Flint / PPG product. HUBSS is the Canadian distributor. NOTE: legacy PDFs reference Quest Construction Products, the previous brand owner.

PURPOSE OF THIS DOCUMENT

Source-of-truth reference for HUBSS website product copy. Replaces existing website descriptions that have been flagged as inaccurate or embellished. Doug Bain to review, correct, and sign off — every claim on the website must be supported by a fact listed in this document.

## What it is

A high-performance waterborne epoxy-modified acrylic pavement coating that turns ordinary asphalt or concrete into coloured, durable, slip-resistant surfaces — bike lanes, bus priority lanes, decorative crosswalks, plazas, parks, and branded private installations.

StreetBond is a system, not a single product. The line includes water-based variants (SB120, SB150, SB150 AL), MMA-based variants for cold-climate work (Pro 220, Pro 250), and concrete primers (QS solvent-based, WB waterborne).

## Key features

- Waterborne epoxy-modified acrylic — flexes with the pavement, resists peeling, balances hardness against wear and slip.

- 73+ standard colours plus custom colour matching. 'Invisible Shade' technology pushes Solar Reflectance above 0.334 even on darker colours.

- ADA-compliant.

- VOC < 50 g/L (calculated) for the water-based variants — well below SCAQMD Rule 1113 limits for industrial maintenance coatings.

- 1-year limited manufacturer warranty (additional coverage available for eligible projects).

- Documented field performance: 10+ years on Beale Street (Memphis); 12+ years in Padua (Italy).

## Technical specifications

| Product family | SB120 + SB150 + SB150 AL (water-based, epoxy-modified acrylic); Pro 220 + Pro 250 (MMA / PMMA); Concrete Primer QS + WB |
| --- | --- |
| Chemistry (water-based) | Two-component waterborne epoxy-modified acrylic (Part A + Part B + colourant) |
| Density | SB120: 14.0 lb/gal (1.67 g/mL); SB150: 13.7 lb/gal (1.65 g/mL); SB150 AL: 11.1 lb/gal |
| Volume solids | SB120: 54–61%; SB150: 53.5–60.6%; SB150 AL: 45.2 ± 2% |
| VOC | < 50 g/L (calculated) for water-based variants |
| Drying — touch dry | 1–4 hours at 77°F (25°C), 40% RH (ASTM D5895) |
| Cure — to traffic | 6–24 hours (climate dependent) |
| Application temperature | 50°F (10°C) and rising, up to 113°F (45°C). Surface temp must be 50°F and rising. No precipitation within 24 hours. |
| Coverage (single layer, sprayed) | ≈ 600 ft² per 5-gal unit at 6.3 mil dry thickness (≈ 146 ft²/gal) |
| Coverage (3 layers, pedestrian) | ≈ 200 ft² per unit (≈ 49 ft²/gal) |
| Coverage (4 layers, vehicular) | ≈ 150 ft² per unit (≈ 36 ft²/gal) |
| Friction — SB150 (ASTM E303) | Dry 55–90 BPN / Wet 35–70 BPN |
| Taber abrasion — SB150 (H-10 wheel) | 0.16–1.0 g per 1,000 cycles (dry) |
| Adhesion (ASTM D4541) | 300–1,400 psi |
| Freeze point | 32°F (0°C) — do not let pail freeze |
| Pro 220 / 250 application temp | 32°F to 95°F (0–35°C); rain-proof in ~30 min at 68°F (20°C) |

## Colours / palette

73+ standard colours plus full custom colour matching. Standard tile palette includes Traffic Red, Bike Lane Green, Sunflower, Pacific Blue, Civic Orange, Night White. SR-qualifying colours are flagged in the StreetBond Colour Guide. 'Invisible Shade' technology pushes Solar Reflectance above 0.334 on darker tones.

## Applications & ideal use-cases

- Bike lanes and cycle priority zones

- Bus priority lanes and BRT station zones

- Decorative coloured crosswalks

- Civic plazas and pedestrian-priority surfaces

- Parks and pathway surfacing

- Branded private driveways and entryways

- Sport courts and playground surfacing

- Parking lots and parking-stall delineation

## Document library

Current document set for this product. Proposed clean titles below — fixes duplicate / generic naming on the current site.

| Document title | Type | File |
| --- | --- | --- |
| StreetBond Brochure | Brochure | StreetBond-Brochure.pdf |
| StreetBond Colour Guide (73+ colours) | Colour Guide | StreetBond-Colour-Guide.pdf |
| Substrate Preparation Guide | Substrate | StreetBond_Substrate_Guide.pdf |
| Colorant Technical Data Sheet | TDS | StreetBond-Colorant.pdf |
| SB120 — Technical Data Sheet | TDS | StreetBond-SB120-Data-Sheet-12.22-Rev.pdf |
| SB120 — Product Specification (asphalt) | Specification | StreetBond_SB120_Specifications.pdf |
| SB120 — Product Specification (over concrete) | Specification | StreetBond-SB120-Over-Concrete-Specification.pdf |
| SB150 — Technical Data Sheet | TDS | StreetBond-SB150-Data-Sheet-12.22-Rev.pdf |
| SB150 AL — Technical Data Sheet (airless sprayer compatible) | TDS | StreetBond-SB150AL-Data-Sheet-12.22-Rev.pdf |
| SB150 — Product Specification (asphalt) | Specification | StreetBond_SB150_Specifications.pdf |
| SB150 — Product Specification (over concrete) | Specification | StreetBond-SB150-Over-Concrete-Specification.pdf |
| Pro 220 (MMA) — Technical Data Sheet | TDS | StreetBond-Pro-220-TDS.pdf |
| Pro 220 + 250 — Installation Guide | Installation | StreetBond-Pro-220-and-250-Intallation.pdf |
| Pro 220 + 250 — Brochure | Brochure | StreetBond-Pro-220-Pro-250-Brochure-1.pdf |
| Pro 250 (PMMA) — Technical Data Sheet | TDS | Data-Sheet-StreetBond-Pro-250.pdf |
| Concrete Primer QS — Technical Data Sheet (solvent-based) | TDS | StreetBond-QS-Concrete-TDS.pdf |
| Concrete Primer WB — Technical Data Sheet (waterborne) | TDS | StreetBond-Concrete-Primer-WB-TDS.pdf |

## Source notes & [VERIFY] flags

SOURCES USED

- StreetBond Brochure, Colour Guide, Substrate Guide (.pdf)

- StreetBond SB120 / SB150 / SB150 AL Technical Data Sheets (.pdf)

- StreetBond Pro 220 and Pro 250 Technical Data Sheets (.pdf)

- StreetBond Concrete Primer QS + WB Technical Data Sheets (.pdf)

ITEMS REQUIRING DOUG'S CONFIRMATION

[VERIFY] Manufacturer attribution: confirm whether HUBSS website should attribute StreetBond to GAF, to 'StreetBond by GAF,' or simply present it as a product family without manufacturer attribution. Current site says nothing about GAF.

[VERIFY] "Pantone matching" claim: the StreetBond brochure mentions custom colours and 73+ standard colours; it does not explicitly state "full Pantone matching." Pantone PMS codes ARE published on TrafficPatterns/TPXD colour guides, but not on StreetBond. Confirm with HUBSS whether the Pantone-match claim is supportable for StreetBond specifically.

[VERIFY] Site "30–50 sq ft per gallon" — defensible at the 3–4 layer level but only meaningful with a layer-count qualifier. Recommend wording: "Coverage 36–49 ft²/gal at 3–4 layer build (pedestrian / vehicular)."

[VERIFY] Site "2–4 hours dry time" — accurate as TOUCH-DRY, but cure-to-traffic is 6–24 hours. Recommend separating: touch-dry 1–4 hr, cure-to-traffic 6–24 hr.

[VERIFY] Manufacturer line attribution: legacy PDFs still carry 'Quest Construction Products' branding while newer TDSs read 'StreetBond by GAF.' Confirm with the supplier which branding should appear on the HUBSS website.

CURRENT SITE COPY FLAGGED AS INACCURATE / EMBELLISHED

[VERIFY] Current site is silent on manufacturer attribution. StreetBond is a GAF/StreetBond product, not an Ennis-Flint/PPG product. This matters because GAF and PPG are different companies — and Doug is likely to be asked about it by spec writers.

[VERIFY] Current site lists 'Pantone matching' as a spec. Pantone reference values are published for TrafficPatterns colours, not for StreetBond — the StreetBond colour guide uses StreetBond's own colour codes. Update the spec to '73+ standard colours plus custom colour-matching capability' until Pantone is verified.

Approved for website use by: ______________________________   Date: ______________