FLAGSHIP — STAMPED ASPHALT SYSTEM

# StreetPrint

Manufacturer: Integrated Paving Concepts (IPC) — originator of the StreetHeat® reciprocating asphalt re-heating technology. The colour coat is StreetBond150 (GAF). HUBSS is the Canadian certified-applicator network.

PURPOSE OF THIS DOCUMENT

Source-of-truth reference for HUBSS website product copy. Replaces existing website descriptions that have been flagged as inaccurate or embellished. Doug Bain to review, correct, and sign off — every claim on the website must be supported by a fact listed in this document.

## What it is

A genuine stamped-asphalt system. The asphalt itself is reheated in place with StreetHeat® infrared equipment, imprinted with a wire-rope template using a vibratory plate compactor, then coated with StreetBond150 for colour and protection.

The finished surface IS the asphalt — there is no separate paver, no thermoplastic inlay, no joints. This makes the surface flush with the surrounding road and structurally compatible with municipal winter maintenance.

## Key features

- Surface is the asphalt itself — imprinted, not a separate material laid on top.

- Flush with surrounding pavement — no raised edges, no shear risk under snowplow blades.

- More than 50 million square feet installed since 1992 (manufacturer claim).

- 100+ template SKUs across 15 pattern families: Offset Brick, Diagonal Herringbone, Standard Herringbone, Ashlar Slate, British Cobble, Stone, Eurofan, Scallop, Tile sets, Borders, Accents, Radial Extensions, Numbers/Letters, Signage/Playground, International.

- Colour comes from StreetBond150 — full 73+ colour StreetBond palette available.

- Left uncoated, the imprinted asphalt can be opened to traffic immediately.

- Must be installed by a certified StreetPrint applicator. HUBSS maintains the Canadian applicator certification.

## Technical specifications

| System | Imprinted asphalt + StreetBond150 colour coat |
| --- | --- |
| Imprint depth | Minimum 3/8 inch — areas less than 3/8" must be reheated and re-stamped |
| Asphalt heating depth | Minimum 1/2 inch (12.5 mm) without burning the surface |
| Surface temperature limit during heating | Must not exceed 325°F (162°C) by infrared measurement |
| Recommended HMA thickness | 1.5–2 inches compacted. 1" asphalt risky (grout-line cracking) |
| Open to traffic — uncoated | Immediately |
| Open to traffic — coated | Per StreetBond150 cure schedule: 6–24 hours |
| Pattern library | 15 families, 100+ individual template SKUs |
| Template sizes | SR-120, SR-60, SR-20 (proprietary); paver-compatible options |
| Substrate | Asphalt only — not for patios, pool decks, or concrete surfaces |
| Warranty on imprint itself | None — variables outside manufacturer control (traffic, asphalt mix, install quality). Coating carries StreetBond warranty. |

## Colours / palette

Full StreetBond150 colour palette — 73+ standard colours plus custom. SR-qualifying tones available for LEED projects (use the StreetBondSR specification when SR is required).

## Applications & ideal use-cases

- Decorative crosswalks on asphalt

- Residential and commercial driveways

- Parks, pathways, and trails

- Plazas and pedestrian-priority streetscapes

- Town home developments and community-branding installations

- Heritage district streetscape recreations (brick, cobble, slate, fan patterns)

- Traffic-calming installations and gateway treatments

- Public art installations using custom templates

## Document library

Current document set for this product. Proposed clean titles below — fixes duplicate / generic naming on the current site.

| Document title | Type | File |
| --- | --- | --- |
| StreetPrint FAQ | FAQ | StreetPrint-FAQ.pdf |
| Asphalt Texturing Specification | Specification | StreetPrint-Asphalt-Texturing-Specification.pdf |
| Colour Guide | Colour Guide | StreetPrint-Colour-Guide.pdf |
| Template Catalog (100+ pattern SKUs) | Template Catalog | StreetPrint-Template-Catalog.pdf |

## Source notes & [VERIFY] flags

SOURCES USED

- StreetPrint Asphalt Texturing Specification (.pdf)

- StreetPrint FAQ (.pdf)

- StreetPrint Template Catalog (.pdf)

- StreetPrint Colour Guide (.pdf)

ITEMS REQUIRING DOUG'S CONFIRMATION

[VERIFY] Current site claims "12+ standard patterns." The Template Catalog shows 100+ SKUs across 15 families. Recommend updating to "100+ patterns across 15 families."

[VERIFY] "Snowplow-safe" — the flush-surface design absolutely is plow-tolerant in practice, but no PDF reviewed uses the exact phrase "snowplow-safe." Confirm with HUBSS that this is the right shorthand to use on the website.

[VERIFY] "More than 50 million square feet installed since 1992" — manufacturer marketing claim. Confirm whether HUBSS wants to use this number or a Canada-specific figure.

[VERIFY] The original product is sometimes referred to as just "StreetPrint" and sometimes as "StreetPrint Genuine Stamped Asphalt." Confirm preferred product name for site copy.

CURRENT SITE COPY FLAGGED AS INACCURATE / EMBELLISHED

[VERIFY] Current site says "12+ standard patterns plus fully custom designs." Significantly understated — the Template Catalog includes 100+ SKUs in 15 pattern families. Easy fix and a stronger marketing claim.

Approved for website use by: ______________________________   Date: ______________