SPECIALTY — ASPHALT MAINTENANCE COATING

# DuraShield

Manufacturer: GAF / StreetBond (Parsippany NJ). DuraShield is a StreetBond family product, NOT an Ennis-Flint / PPG product. HUBSS is the Canadian distributor.

PURPOSE OF THIS DOCUMENT

Source-of-truth reference for HUBSS website product copy. Replaces existing website descriptions that have been flagged as inaccurate or embellished. Doug Bain to review, correct, and sign off — every claim on the website must be supported by a fact listed in this document.

## What it is

A two-component waterborne epoxy-modified acrylic pavement maintenance coating, spray + back-roll applied to asphalt. Used for parking lots, residential driveways, and pedestrian areas where colour, slip resistance, and chemical protection are required — but the heavy decorative finish of StreetBond150 isn't needed.

Available in two documented colour variants: Asphalt (black) and Solar Gray. Solar Gray provides solar reflectance for heat-mitigation projects.

## Key features

- Same flexible epoxy-modified acrylic chemistry as StreetBond — moves with the pavement, will not peel.

- Solar Gray variant: Solar Reflectance = 0.33, contributes to heat-island mitigation.

- VOC < 50 g/L — well below SCAQMD Rule 1113 thresholds for industrial maintenance coatings.

- Excellent chemical resistance — manufacturer cites resistance to UV damage; per-chemical fuel/oil/deicing-specific resistance data is not enumerated in the TDS.

- Available with anti-slip aggregate broadcast for pedestrian areas (a field practice, not enumerated in the two TDS files reviewed).

- 24-month shelf life unopened (40°F–90°F).

## Technical specifications

| Type | Two-component waterborne epoxy-modified acrylic |
| --- | --- |
| Density | 14.3 lbs/gal (1.7 kg/L) per ASTM D1475 |
| Volume solids | 57% (±2) per ASTM D2697 |
| Weight solids | 75% (±2) per ASTM D2369 |
| Shore hardness | 80.8 (ASTM D2240) |
| Mandrel bend | 1-1/2 in @ 23°C per ASTM D522-93 A |
| Water absorption | < 6% (ASTM D570) |
| VOC | < 50 g/L (calculated) |
| Solar Reflectance (Solar Gray variant) | SR = 0.33 initial |
| Coverage | 65 sq ft/gallon (1.6 m²/L), 25 mil wet / 14 mil dry, in 2 layers |
| Taber abrasion — dry (H-10 wheel) | 0.7 g per 1,000 cycles per ASTM D4060 |
| Taber abrasion — wet (H-10 wheel) | 3 g per 1,000 cycles |
| Friction — dry | > 65 BPN per ASTM E303 |
| Friction — wet | > 35 BPN per ASTM E303 |
| Drying — touch dry | 35 min at 73°F (23°C), 37% RH (ASTM D5895) |
| Minimum install temperature | 50°F (10°C) and rising; not to drop below 50°F within 24 hours |
| Packaging | Part A 5-gal (3.75 gal net) + Part B 1-pint (10 oz net); OR Part A 55-gal drum + Part B 2-gal |
| Substrate | Asphalt (per the two TDS sheets reviewed) |

## Colours / palette

Two documented colours per the TDS sheets: Asphalt (black) and Solar Gray. Per TDS, colour "cannot be altered using supplemental pigments." Other colours may exist in the broader DuraShield line — verify with the manufacturer if expanded palette claims are needed on the site.

## Applications & ideal use-cases

- Parking lots — asphalt restoration and protection

- Residential driveways — paving and asphalt maintenance

- Pathways, raised medians, pedestrian plazas

- Pedestrian areas (anti-slip aggregate broadcast option)

- Asphalt surfaces exposed to chemicals (fuel, oil, deicers) — per manufacturer claim

- Heat-mitigation surfaces (Solar Gray variant for parking lots and large hardscape)

## Document library

Current document set for this product. Proposed clean titles below — fixes duplicate / generic naming on the current site.

| Document title | Type | File |
| --- | --- | --- |
| Part A+B Asphalt (black) — Technical Data Sheet | TDS | DuraShield-Pavement-Coating-Part-A-B-Color-Asphalt-TDS.pdf |
| Part A+B Solar Gray — Technical Data Sheet | TDS | DuraShield-Pavement-Coating-Part-A-B-Color-Solar-Gray-TDS.pdf |

## Source notes & [VERIFY] flags

SOURCES USED

- DuraShield Asphalt (black) Part A+B Technical Data Sheet (.pdf)

- DuraShield Solar Gray Part A+B Technical Data Sheet (.pdf)

ITEMS REQUIRING DOUG'S CONFIRMATION

[VERIFY] Current site says SR = 0.34. The TDS documents SR = 0.33. Recommend correcting to 0.33.

[VERIFY] Current site says "low VOC, meets SCAQMD regulations." The TDS lists VOC < 50 g/L — defensible as meeting SCAQMD Rule 1113 limits, but the TDS itself does not explicitly cite SCAQMD certification. Recommend revising to "Low VOC (< 50 g/L) — meets typical industrial maintenance coating limits."

[VERIFY] Current site says "fuel/oil/deicing resistant." The TDS lists "Excellent chemical resistance" generically and "Highly resistant to UV damage," but specific fuel/oil/deicing-resistance test results are not enumerated. Confirm with manufacturer or soften to "chemically resistant per manufacturer."

[VERIFY] Current site says "anti-slip available with aggregate texture." This is a standard field practice but is not documented in the two TDS sheets reviewed. Confirm whether DuraShield has a defined anti-slip add-mix or whether this is broadcast aggregate (field decision).

[VERIFY] Manufacturer attribution: confirm whether the HUBSS website should attribute DuraShield to GAF / StreetBond, or present it as a HUB Surface Systems product without manufacturer attribution. The TDS is a GAF/StreetBond document.

CURRENT SITE COPY FLAGGED AS INACCURATE / EMBELLISHED

[VERIFY] Site spec says Solar Reflectance = 0.34. The Solar Gray TDS clearly states SR = 0.33 initial. Easy correction.

[VERIFY] Site claim of SCAQMD compliance is not directly supported by the TDS, which only lists VOC < 50 g/L. The two facts are consistent but not equivalent.

[VERIFY] Site claim of fuel / oil / deicing resistance is more specific than the TDS supports. The TDS uses the generic phrase "excellent chemical resistance." Per-chemical test data would need to come from the manufacturer.

Approved for website use by: ______________________________   Date: ______________